## Slide 1: RSS Collimator Repair
What are we doing to fix it.
We = Darragh Eric Francois Jonathan Lisa Martin Vic and Myself

## Slide 2: RSS Collimator Repair
Collimator
Field Lens
Fused Quartz, CaF2, LL3421, Sylgard, Throughput Failure.
Triplet
CaF2, NaCl, LL3421, Sylgard, Throughput Failure.
Doublet
Fused Silica, CaF2, LL5610, Sylgard, Coating Failure? Sylgard Failure?
Dispersive Elements
Beam Splitter
Calcite, LL5610, Sylgard, Sylgard Failure.
Camera
Quadruplet
Fused Silica, CaF2, LL5610, Sylgard, Throughput OK, Is the Sylgard Failing?
Triplet
Fused Silica, NaCl, LL5610, Sylgard Throughput OK,
Is the Sylgard Failing?

## Slide 3: RSS Collimator Repair
Project in a re-definition phase.
Does LL3421 damage the lens surfaces?
  No – Oil change maintenance till we find culprit material.
  Yes – Dump fluid and change opto-mechanical design
Is Sylgard and LL5610 compatible?
  No – Dump fluid and figure what to do about the camera
  Yes – Figure out why there is a bubble in the doublet.
Do we need to dump fluid coupling?
  LL3421, LL5610 or both?

## Slide 4: How do we answer these Questions
Remove RSS
Measure through put of individual lens groups
  Before and after an oil change
  See if lens surfaces are damaged
Inspect Doublet Bond
  Determine if Bond is failing.
Compare the fluid from the Doublet to the Camera Fluid.
  Does the reaction with Sylgard leave a tell tale trace?
What do we do when the test are inconclusive?